Canopy tinting with Rite Dye:

Author unknown

1. Clean your canopy with soap/water, rinse and let dry. Handle only on the edges after that. 
2. Mix 2 parts black Rite Dye powder with 1 part navy blue. Using only straight black will give you a BROWN tint! 
3. Have a container large enough to completely cover your canopy. 
4. Have a second container of rinse water ready or at least some way to rinse the canopy off. 
5. Buy a cheap candy thermometer (or steal your wife's) I take no responsibility!! 
6. Have your container in an area where it doesn't matter if you spill!! You will spill, splatter or drip! 
7. Heat your water to about 150 degrees. Note, a large thin canopy might not stand higher temps! 
8. Wait until the water temperature in your container totally stabilizes, it may still be rising from hotter water in the bottom. 
9. Thoroughly mix in the dye. 
10. Plunge the canopy into the mix with one movement. Any hang up during this process could create a faint line of differing tint. 
11. Use a pliers or tongs to bring it out. If not dark enough, put it back in(see #10 and see below). 
12. Bring canopy out, immediately rinse and place in a clean area to dry. 
13. Dispose the dye water in a safe area??? Hot water will kill the lawn. 

I tried Russ Brandt’s method as stated below except I still heated the water and only used about 2 tablespoons of vinegar in my staining bucket. I was tinting a Great Planes CAP 232 and GP Ultimate canopies. The results were significantly darker than what I am used to, but they do look very nice. His method is very effective if you want a dark canopy. Also the canopies were somewhat “relaxed” around the edges after experiencing 150 degree heat. They were not misshapen, just loose around the base. If you only want a slight tint then I would recommend omitting the vinegar.

___________________________________________________________________________________


HERE IS THE ALTERNATE METHOD USING VINEGAR BY Russ "MT" Brandt 


Canopy tinting with Rite Dye: 
1. Clean your canopy with soap/water and dry. Handle only on the edges after that. 
2. Mix 2 parts black Rite Dye with 1 part navy blue. Straight black will give you a BROWN tint. 
3. Have a container large enough to completely cover your canopy. 
SKIP #5 
5. Have your container in an area where it doesn't matter if you spill!! 
SKIP #7 & 8 Use hot tap water & add 25% white vinegar. 
8. Thoroughly mix in the dye, and the vinegar. 
9. Plunge the canopy into the mix with one movement. Any hang up could create a faint line of differing tint. 
10. Use a pliers or tongs to bring it out. If not dark enough, put it back in  (see #9). 
11. Bring canopy out, rinse in clean water and place in a clean area to dry. 
12. Dispose the dye water in a safe area???